PART 1 – GENERAL

  - DESCRIPTION

- StreetBond® Advanced Coatings for Asphalt are specifically formulated for application to asphalt pavement and have been confirmed by a certified testing facility to possess a balance of performance properties for a durable and color-fast finish.

- A variety of StreetBond® coating colors are available. Please refer to gaf.com to view these. Custom colors are available upon request.

- Certain colors of the StreetBond® coatings have been independently verified to have an SRI greater than 29 and therefore can help projects qualify for points in the LEED® program under Heat Island Effect: Non-Roof. Please refer to gaf.com for further information.

- Qualifications. Only Accredited StreetBond® Applicators may bid for and perform the imprinted portion of this work. Please refer to Section 1.3 DEFINITIONS.

- StreetBond® products are manufactured in ISO 9001:2008 / ISO 14001:2004 facilities to ensure quality products produced in legally-responsible and environmentally-
conscious manner.

- StreetBond® coatings are only available from GAF.

1.2 REFERENCES

| - ASTM D4541 | Standard Test Method for Pull-Off Strength of Coatings Using Portable Adhesion Tester. |
| --- | --- |
| - ASTM D4060 | Test Method for Abrasion Resistance of Organic Coatings by the Taber Abraser. |
| - ASTM D2697 | Standard Test Method for Volume of Nonvolatile Matter in Clear or Pigmented Coatings. |
| - ASTM D522-93A | Standard Test Method for Mandrel Bend Test of Attached Organic Coatings. |
| - ASTM D1653 | Standard test method for water vapor transmission through organic film coatings. |
| - ASTM G154 | QUV Accelerated Weathering Environment. Standard Practice for Operating Fluorescent Light Apparatus for UV Exposure of Nonmetallic Materials. |
| - ASTM D2369 | Weight Solids Standard test method for Volatile Content of Coatings. |
| - ASTM D1475 | Standard Test method for Density of Paint, Varnish, Lacquer, Other related products. |
| - ASTM D2240 (2000) | Standard Test Method for Rubber property – Durometer hardness. |
| - ASTM D5895 | Standard Test Method of drying or curing during film formation of organic coatings using mechanical recorders. |
| - ASTM D570 | Standard Test Method for water absorption of plastics. |

1.3 DEFINITIONS

- “Accredited StreetBond® Applicator” has valid Certification for both Textured (stamped) and Non-Textured (flatwork) as offered by GAF and are reviewed on an annual basis.  All Accredited StreetBond® Applicators have been qualified by GAF to perform the Work and offer a product Warranty.

- “Approved Applicator” has valid Certification for non-textured (flatwork) application ONLY as offered by GAF and are reviewed on an annual basis.  Product Warranties may be available to Approved Applicators but require approval and supervision by a GAF Technical Sales Representative.

- “Applicator” means the installer of the StreetBond® coatings.

- “Owner” means the Owner and refers to the representative person who has decision making authority for the Work.

- “TSR” is a GAF Technical Sales Representative who manages the StreetBond® product in a given territory.

- “Stamped asphalt pavement” is asphalt pavement that has been subjected to imprinting or texturing in a specific pattern.

- “Non-Stamped asphalt pavement” is asphalt pavement that is unstamped and is sometimes referred to as “flatwork”.

- The “Work” is the asphalt pavement texturing work contemplated in this bid submission and specification.

- “Scuffing” is a “tear” of the asphalt pavement caused by an external force – for example turning the steering wheel of a stationary vehicle.  Scuffing is generally the result of poorly designed or improperly installed asphalt and would most-commonly be seen on weaker residential asphalt.

- “Layer” is a signal thin pass of coating, applied with a texture spray gun, which is allowed to dry before the next layer is applied.

1.4 SUBMITTALS

A copy of the Accreditation Certificate, available from the Applicator, is required with submittal. Independent test results available upon request.

PART 2 – PRODUCTS

2.1 MATERIALS – STREETBOND® COATINGS

StreetBond® coatings have been scientifically formulated to provide the optimal balance of performance properties for a durable, long-lasting color and textured finish to asphalt pavement surfaces.  Some of these key properties include wear and crack resistance, color retention, adhesion, minimal water absorption and increased friction properties.  StreetBond® coatings are environmentally safe and meet EPA requirements for Volatile Organic Compounds (VOC).

A. StreetBond® SB120 is a premium epoxy-modified, acrylic, waterborne coating specifically designed for application on asphalt pavements.  It has a balance of properties to ensure good adhesion and movement on flexible pavement, while providing good durability.  StreetBond® SB120 is durable in both dry and wet environments. StreetBond® SB120 is specifically designed for pedestrian and residential use. It should not be used in 
vehicular applications.

B.	StreetBond® SR Colorant is a highly concentrated, high quality, reflective, UV stable pigment blend designed to add a solar reflectance color to StreetBond® SB120 coatings. One unit of SR Colorant shall be used with one pail of StreetBond® coating material..

2.1.1 Properties of StreetBond® coatings

The following tables outline the test results for physical and performance properties of the StreetBond® coatings as determined by an independent testing laboratory.

TABLE 1: Typical Physical Properties of StreetBond® Coatings

| Characteristic | Test Specification | SB120 |
| --- | --- | --- |
| Solids by Volume | ASTM D-2697 | 57.0% |
| Solids by Weight | ASTM D-2369 | 74.7% |
| Density | ASTM D-1475 | 14.0 lbs/gal ( 1.67kg/l) |

TABLE 2: Typical Performance Properties of StreetBond® Coatings

| Characteristic | Test Specification | SB120 |
| --- | --- | --- |
| Dry time (To re-coat) | ASTM D5895 23°C; 37% RH | 35 min |
| Taber Wear Abrasion Dry H-10 wheel | ASTM D4060 8 day cure | 0.03 g/1000 cycles |
| Taber Wear Abrasion Wet H-10 wheel | ASTM D4060 7 days cure | 0.68 g/1000 cycles |
| QUV Accelerate Weathering Environment | ASTM G-151 ΔE 1,500hrs. | 0.76 (Brick) |
| Hydrophobicity Water Absorption | ASTM D471 | 10.272% |
| Shore hardness | ASTM D2240 | 42.3 |
| Mandrel Bend | ASTM D522-93A | 1/4” @ 21° C |
| Permeance | ASTM D1653 | 13.43g/m²/ 24hr/mmHg (52 mils) |
| VOC | per MSDS | 17 g/l |
| Adhesion to Asphalt | ASTM D4541 | > 300 psi (1980 psi) |
| Friction | ASTM E303 British Pendulum Tester | Wet=66 Dry=88.3 |

Certificates of Analysis are available upon request for each of these properties.

2.2 EQUIPMENT FOR STREETBOND® APPLICATION

The equipment described has been designed specifically for optimal application of StreetBond® coatings. Other equipment may or may not be suitable and could compromise the performance of the StreetBond® coatings and/or reduce crew productivity.

- The SB Flex Sprayer is a proprietary coating sprayer supplied by Intech Equipment and is capable of applying the StreetBond® coatings to the asphalt pavement surface in a thin, controlled film which will optimize the drying and curing time of the coating. A Graco RTX and RapidSprayerII sprayer may also be used.

- The StreetBond® Coatings Mixer is a motorized mixing device designed to ensure efficient and thorough blending of the StreetBond® components.

- Backpack or Hand-Held sprayer to apply the diluted StreetBond® Adhesion 
Promoter Concentrate.

- The RapidFinisher II is an electric powered broom produced by Integrated Paving Concepts Inc. that can be used in the application of StreetBond® coatings to improve productivity.  It is especially useful on larger projects.

PART 3 – EXECUTION

3.1 GENERAL

StreetBond® coating shall be supplied and applied on non-textured asphalt surface by an Accredited StreetBond® Applicator in accordance with the plans and specifications or as directed by the Owner.  Do not begin installation without confirmation of an Accreditation Certificate. Specifications for the execution of the StreetPrint® system can be found at gaf.com.

3.2 PRE-CONDITIONS

The condition of the asphalt substrate will impact the performance of the StreetBond® coatings.  A highly stable asphalt pavement free of defects is recommended.

3.2.1 Pre-requisites for new asphalt pavement

A durable and stable asphalt pavement mix design installed according to best practices over a properly prepared and stable substrate is a pre-requisite for all long-lasting asphalt pavement surfaces.  The application of StreetBond® does not change this requirement.

3.2.2 Pavement Marking Removal: recommended guidelines

Pavement markings may be removed by sandblasting, water-blasting, grinding, or other approved mechanical methods. The removal methods should, to the fullest extent possible, cause no significant damage to the pavement surface.

The Owner shall determine if the removal of the markings is satisfactory for the application of StreetBond® coatings.   Work shall not proceed until this approval is granted.

3.2.3 Surface Preparation

The asphalt pavement surface shall be dry and free from all foreign matter, including but not limited to dirt, dust, de-icing materials, and chemical residue.

3.3   APPLICATION OF STREETBOND® COATINGS

3.3.1 Coating Application Guidelines

- The Applicator shall use the SB Flex Spray System or suitable texture coatings sprayers to apply the StreetBond® coatings.

- The asphalt pavement surface shall be completely dry and thoroughly cleaned prior to application of the coatings.

- The coating application shall proceed as soon as practical upon completion of the imprinting of the asphalt pavement where applicable.

- For polished asphalt, StreetBond® Adhesion Promoter should be applied directly to the asphalt and allowed to dry completely prior to the first layers of coating.

- For concrete surfaces, StreetBond® WB Concrete Primer should be applied and allowed to cure prior to the first layers of coating. Please consult Technical Data sheets for more details on applications.

- The first layer of coating shall be spray applied then broomed to work the coating material into the pavement surface.  Subsequent applications shall be sprayed then broomed or rolled.  Each application of coating material shall be allowed to dry to the touch before applying the next layer.

- The Applicator shall apply the StreetBond® coatings only when the air temperature is 50°F (10°C) and rising and will not drop below 50°F (10°C) within 24 hours. No precipitation should be expected within 24 hours.

3.4 COATING COVERAGE & THICKNESS

Coating coverage and thickness is as outlined in TABLE 4 below.  Actual coverage may be affected by the texture of the asphalt pavement substrate and the imprint pattern selected.  There will be less coverage with the first layer and higher coverage with subsequent layers.

TABLE 4: COATING COVERAGE AND THICKNESS

|  | COVERAGE (approx.) |  | THICKNESS (approx.) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| # OF LAYERS | NON-TEXTURED |  | WET |  | DRY |  |
|  | sqft/unit* | sqm/unit* | mm | mil | mm | mil |
| 3 | 200 | 18.6 | 0.84 | 33 | 0.48 | 19 |
| 4 | 150 | 13.9 | 1.12 | 44 | 0.66 | 26 |

*1 unit is a nominal 5 gallon pail comprising Part A, Part B and Colorant (approximately 4.12 gallons). 1 unit when sprayed as a single layer covers approximately 600sqft (55.7 sqm), with an approximate thickness of 6.3mil (0.16mm) dry.

3.5 RECOMMENDED COATING COVERAGE RATES

Please check with GAF in advance to confirm the recommended application for the climate conditions at the project location.

TABLE 5: RECOMMENDED COATING COVERAGE RATES

|  | Hot Dry Climate | Temperate/Winter Climate |
| --- | --- | --- |
| Application |  |  |
| Pedestrian only | 3 layers at 600 ft2 (56m2) per 5 gallon (20 Litre) unit for a net coverage of 200 ft2 (18.6m2) per 5 gallon (20 Litre) unit | 3 layers at 600 ft2 (56m2) per 5 gallon (20 Litre) unit for a net coverage of 200 ft2 (18.6m2) per 5 gallon (20 Litre) unit |
| Residential driveway | 3 layers at 600 ft2 (56m2) per 5 gallon (20 Litre) unit for a net coverage of 200 ft2 (18.6m2) per 5 gallon (20 Litre) unit | 3 layers at 600 ft2 (56m2) per 5 gallon (20 Litre) unit for a net coverage of 200 ft2 (18.6m2) per 5 gallon (20 Litre) unit |

- A maintenance program may be required for applications exposed to:

- abrasive materials (such as salt and sand)

- abrasive equipment (such as snow removal equipment)

- Studded winter tires

3.6   OPENING TO TRAFFIC

Minimally, StreetBond® SB120 coating must be 100% dry and sufficient curing time must be allowed before traffic is permitted on the surface.

TABLE 6: COATING DRY TIMES (TYPICAL)

If StreetBond® coatings are applied when moisture cannot evaporate, then the coating will not dry. The drying and curing of StreetBond® coatings have a direct impact on performance.

PART 4 – MEASUREMENT AND PAYMENT

4.1 MEASUREMENT

The measured area is the actual area of asphalt pavement where StreetBond® has been applied, measured in place. No deduction will be made for the area(s) occupied by manholes, inlets, drainage structures, bollards or by any public utility appurtenances within the area.

4.2 PAYMENT

Payment will be full compensation for all work completed as per conditions set out in the contract.  For unit price contracts, the payment shall be calculated using the measured area as determined above.